## Slide 1: Rietveld Refinement Method
ACERS workshop on Tools for Visualizing and Understanding the Structure of Crystalline Ceramics
Taylor Sparks
Professor of Materials Science & Engineering, University of Utah

## Slide 2: Overview
What is it and how does it work?
Quantitative analysis of multiple phases mixture
  Amorphous content
Atomic position & site occupancy
Thermal displacement parameters
Preferred orientation
Crystallite size/strain

## Slide 3: First, lets identify the software we use
Notes: https://advancedphotonsource.github.io/GSAS-II-tutorials/index.html
http://users.uoi.gr/nkourkou/powdll/

## Slide 4: What is Rietveld refinement?
Hugo Rietveld (1969)
Quantitative refinement tool
  Calculated pattern vs measured pattern
  Variable model parameters
  Least-squares refinement
  Account for errors during measurement (shift, zero)
Different from LeBail or Pawley (Profile) fitting
  Ab initio crystal structure determination
http://www.ccp14.ac.uk/poster-talks/rietveld-csiro-axaa-99/rietveld/index.htm

## Slide 5: We can simulate patterns pretty well!

## Slide 6: Intensity of a diffracted peak depends on many parameters!
James R. Connolly, for EPS400-001, Introduction to X-Ray Powder Diffraction, Spring 2010
Notes: I= Intensity of reflection of hkl in phase
I_0= incident beam intensity
r = distance from specimen to detector
lambda= X-ray wavelength
(e^2/mc^2)^2= square of classical electron radius
s = linear absorption coefficient of the specimen
v = volume fraction of phase
Mhkl = multiplicity of reflection hkl of phase
0 = Lorentz-polarization (and monochromator) correction (next to last term to right)
v = volume of the unit cell of phase
2 m = diffraction angle of the monochromator
F(hkl) = structure factor for reflection hkl of phase (i.e., the vector sum of scattering intensities of all atoms contributing to that reflection

## Slide 7: Anomalous Scattering Factors f’ & f” depends on radiation choice
Notes: https://www.xtl.ox.ac.uk/resources/software/fprime.html

## Slide 8: Different instruments yield different peak shape
prism.mit.edu/xray/Rietveld_XRDSimulation.pdf

## Slide 9: Quality of the Fit
Rp is the difference between the observed and the calculated value
Rwp weights the residual so the higher intensity peaks are more important than low intensity ones
Rp or Rwp should be < 10% or χ2 < 4 for a good fit
prism.mit.edu/xray/RietveldGOF.pdf

## Slide 10: Multiple cycles required to find the true global minimum in error
False minimum
True minimum – “global” minimum
Least-squares cycles
Rwp
www.cins.ca/.../APDW08%20Rietveld%20Refinement%20with%20GSAS.ppt
“A Rietveld refinement is never finished, only abandoned” - P.W. Stephens

## Slide 11
Quantitative Analysis of Multiple Phases Mixture

## Slide 12: Quantitative Analysis of Multiple Phases Mixture

## Slide 13: Weight Fraction: “SMZ” Method
S is phase fraction, proportional to number of unit cells measured
M is the molecular weight
Z is the number of formula units per unit cell
SMZ is proportional to the concentration

## Slide 14: How Good is the Quantitive Analysis?
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010
Notes: https://journals.iucr.org/j/issues/2001/04/00/hw0085/hw0085.pdf

## Slide 15: Te Fraction in Seawater Medium
93.9% NaCl
6.1% Te
Rwp = 6.9%
Errors: absorption (transparency), sample volume (more powder)

## Slide 16: Y3Sc4AlO12 Intended Composition
36% YAG (Ia-3d)
50.3% YScO3 (Ia-3)
13.7% YScO3 (Pnma)
Rwp = 5.3%

## Slide 17: Y3Sc5O12 Intended Composition
99.2% Y3/4Sc5/4O3 (Ia-3)
0.8% Y(P63/mmc)
Rwp = 4.7%

## Slide 18: Debye Equation for Amorphous Materials
Need radial distribution function to determine bond distances for analysis
Possible to determine percent amorphous material if standard is added in known amount.
amplitude
distance
vibration

## Slide 19: Diffuse Scattering
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010

## Slide 20: Diffuse Scattering
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010

## Slide 21: Diffuse Scattering
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010

## Slide 22: Diffuse Scattering
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010

## Slide 23: Diffuse Scattering
2 = 1.112
James Kaduk, ICDD, Rietveld Refinement Workshop Oct 2010

## Slide 24: Atomic Position & Site Occupancy
White et al, Structural derivation and crystal chemistry of apatites, Acta Cryst. B, B59 1-16 2003
Gd8+xCa2+y(SiO4)6O2+3x/2+y system
  Anion/cation vacancies
Lab XRD insufficient
  Impurity wt%?
  Volume change?
  Cation site preference?
  Meta-prism twist?

## Slide 25: Atomic Position & Site Occupancy
Stoichiometric composition should have highest thermal conductivity
  Phase separation?
Synchrotron diffraction
  Improved signal to noise ratio
  Improved resolution
  Minimize anomalous scattering
http://www.odec.ca/projects/2005/shar5a0/public_html/mainpage.htm

## Slide 26: Atomic Position & Site Occupancy
Rwp = 6.29%
85% Gd7.7Ca2.3(SiO4)6O2
14% Gd2SiO5
Ca has ~5% on A1
Meta prism twist 23.6o
Initial composition Gd8.333Ca1.5(SiO4)6O2

## Slide 27: Thermal Displacement Parameters
Thermal vibrations quantitatively studied in Rietveld refinement
  Uiso or Uij for anisotropic vibration
Large U values could be due to rattling
  Explanation of RE2SrAl2O7 thermal conductivity?

## Slide 28: Thermal Displacement Parameters
Compostion | La2SrAl2O7 | Nd2SrAl2O7 | Sm2SrAl2O7 | Eu2SrAl2O7 | Gd2SrAl2O7 | Dy2SrAl2O7
Uiso A1 | 0.11(2) | 0.21(5) | 0.40(3) | 0.20(1) | 0.37(3) | 0.96(2)
A1 (P2) occupancy | .73 | .54 | .43 | .32 | .25 | .21
A2 (RS) occupancy | .27 | .46 | .56 | .67 | .72 | .79
Rocksalt layer
Double Perovskite layer
Rocksalt layer
A1 site
CN=12
P2 slab
A2 site CN=9
RS slab

## Slide 29: Preferential Orientation: Sr2Nb2O7
Clearly textured to b-axis, but what is preferred orientation factor?

## Slide 30: Preferential Orientation Sr2Nb2O7
Rwp = 6.9%
Texture index = 5.52
Note: Actual compound had small amount of La3+ doped on Sr2+ site

## Slide 31: Size & Strain
First need to characterize the instrument shape parameters using a standard.
Then use U, V, W to obtain integral breadth for Scherrer’s & Stokes’ equation.
Dv = Kλ/{β cos θ}
ε = β/{4 tan θ}
{βobs − βinst}cos θ = λ/Dv + 4 ε{sin θ}
Williamson-Hall plot
Plot βcos(θ)/λ against 4 sin(θ)
Slope & intercept give size and strain

## Slide 32: Size & Strain
CeO2 before and after micronizing
Volume weighted domain size, Dv, of broadened CeO2 is 226 Å and maximum strain, e is 0.011%

## Slide 33: Summary
Rietveld refinement a valuable quantitative analysis tool for determining…
  Crystal structure information
    atomic positions, thermal displacement parameters, occupancy
  Other information
    Preferred orientation, size, strain, quantitative analysis (including amorphous material)